TRAFFIC AND SAFETY INFORMATIONAL SERIES

FREQUENTLY ASKED QUESTION #5

# Why don’t the painted stripes on the road last longer?

To some motorists it may seem like pavement markings—for example, the stripes on the road that divide lanes of traffic—are reapplied very frequently. The people that apply the stripes to the roads can get pretty frustrated with having to apply and reapply markings. There is no one best material or application technique. Instead, many factors go into the design of pavement markings and the decision of what materials to use and how to apply the markings at each location.

# Durability and cost of materials

When deciding what material to use, durability and cost are evaluated on a case by case basis. Pavement marking materials are generally either paint based or nonpaint based. Paint-based markings are nondurable, lasting from six months to two years. They are relatively inexpensive. Nonpaint-based markings are durable, generally last longer than paint-based markings and are more expensive than paint-based markings. Epoxy is an example of a nonpaint-based marking material..

# Pavement type and condition

The type of pavement surface must also be considered when choosing pavement markings. For example, asphalt concrete surfaces require either hot-applied thermoplastics or heavy applications of paint-based markings in order for the markings to be visible. For streets in good condition, more durable pavement markings are generally used. However, if a street is in poor condition and may be resurfaced soon anyway, one of the less expensive, paint-based materials is usually used.

# Weather and time of year

Paint applied during the summer generally lasts longer than that applied during cold weather. Some nonpaint-based markings are not widely used in Iowa because snow plows have a tendency to remove them.

Amount and kind of traffic

The more traffic on a street, the more quickly markings deteriorate. Trucks and other heavy vehicles typically wear pavement markings more quickly than do passenger cars. Wear and tear will occur, however, even with common use over a period of time. Many factors are considered during pavement marking material and technique decisions, but pavement markings will probably always need to be repaired or reapplied.

For more information

For more information, please contact _________________________.